Photodegradation of thiophene-fullerene solutions

Juraj Chlpík1, Soňa Halászová1, Gabriel Čík2, Július Cirák1

1Faculty of Electrical Engineering and Information Technology,

Slovak University of Technology, Ilkovicova 3, 812 19 Bratislava, Slovakia

2Faculty of Chemical and Food Technology, Slovak University of Technology, Radlinskeho 99, 812 37 Bratislava, Slovakia

juraj.chlpik@stuba.sk

In organic electronic devices conjugated polymers or small organic molecules are widely used as the donor material, whereas fullerene derivatives play a role of acceptors. Heterojunction structure is a basis for the operation of organic solar cells. The photodegradation properties of system oligothiophene-fullerene and polythiofene-fullerene are summarized in the presented work. Fluorescence spectroscopy was used to study the effect of fluorescence quenching after the formation of an excited-state complex between thiophene and fullerene. The formation of excited-state complex in the oligothiophene-fullerene solution was observed even before the exposure. This effect was not evident in the polythiofene-fullerene systems.

Forma prezentácie: poster