PHYSICAL PROPERTiES OF YbPd2In

F. Gastaldo1, A. Džubinská2, M. Reiffers3, I. Čurlik3, M. Giovannini 1

1University of Genoa, Dept. of Chemistry, Genoa, Italy

2Institute of Physics, Faculty of Natural Sciences, P. J. Šafárik University, Košice, Slovakia

3Faculty of Humanities and Natural Sciences, Prešov University, Prešov, Slovakia

marian.reiffers@unipo.sk

The novel compound YbPd2In belonging to the ternary Yb-Pd-In system has been investigated. This work is continuation of our study on R-Pd-X systems (R = Yb, Eu, X = In, Sn). XRD measurements confirmed that it crystallizes in the cubic Heusler Cu2MnAl type structure. We measured the temperature dependence of magnetic susceptibility up to 2 K what shows no magnetic ordering and follows the C-W behaviour. The paramagnetic Curie temperature obtained from the fit is ΘP = -6.3 K, which is an indication of antiferromagnetic exchange interactions. The result of the effective moment for studied system is μeff = 4.05 μB/f.u., which is close to the theoretical value for Yb3+ ion (4.54 μB). Heat capacity was measured from 2 K up to 300 K. At 0 T no anomaly appears and the heat capacity is always decreasing. With an applied magnetic field of 3 T, a maximum in heat capacity develops at 2.5 K. For B > 3 T this maximum shifts and becomes broader. We also measured the temperature dependence of electrical resistivity.

Forma prezentácie: oral