Electronic structure and lattice dynamics of actinide carbides

Lukáš Kývala, Dominik Legut

IT4Innovation Center, VSB-TUO Ostrava, 17. listopadu 15/2172, CZ 708 33 Ostrava, Czech Republic

lukas.kyvala.st@vsb.cz

The actinide carbides can be used as advanced nuclear fuels for the so-called generation IV reactors (including the gas-cooled and sodium-cooled fast reactors). These carbides are promising because of higher thermal conductivity and operational temperature (more efficient heat transfer) over conventional oxide fuels (e.g. UO2). The actinides pose 5f electrons, which are crucial for electronic structure and lattice dynamics. We investigate the effect of spin-orbit interactions, the influence of the localization of 5f electrons on the electronic structures within density functional theory. Next the lattice dynamics (phonons) were calculated within the quasi-harmonic approximation and the phase stability was determined. The localization of 5f electrons was tuned by changing the parameter U, which representing the strong local interactions of the Coulomb type.

Acknowledgments: This work was supported by The Ministry of Education, Youth and Sports from the Large Infrastructures for Research, Experimental Development and Innovations project IT4Innovations National Supercomputing Center LM2015070 and by the grant No. 17-27790S of the Grant Agency of the Czech Republic and by The Ministry of Education, Youth and Sports from the National Programme of Sustainability (NPU II) project ”IT4Innovations excellence in science - LQ1602” and Mobility grant No. MB7847811 and Student Grant Competitions of VSB-TU Ostrava (SP2017/184).

Presentation of contribution: 		poster