Supressed density of states at fermi level in superconducting Boron doped diamond above Tc

O. Onufriienko (a), T. Samuely (a), G. Zhang (c), P. Szabó (a), V.V. Moshchalkov (b) and P. Samuely (a)

Centre of Low Temperature Physics, Institute of Experimental Physics, Slovak Academy of Sciences and Faculty of Science, P.J. Šafárik University, 040 01 Košice, Slovakia (a).

INPAC-Institute for Nanoscale Physics and Chemistry, KU Leuven, Celestijnenlaan 200D, B-3001 Heverlee, Belgium (b).

oleksandr.onufriienko@student.upjs.sk

We present our Scanning tunneling microscopy/spectroscopy (STM/S) study of monocrystalline superconducting boron-doped diamond film prepared by chemical vapor deposition with low doping level. We observe two different temperature regions with clearly distinctive behavior of zero bias conductivity vs. temperature dependence. Below 1 K (bulk Tc value), the behavior is clearly dominated by the thermal suppression of superconductivity. (Fig.1a) However, a V shaped spectrum persists up to temperatures well above the bulk Tc. (Fig.1b) We discuss this phenomenon in terms of Coulomb interactions and other possible effects.

Fig.1: Normalized differential conductance vs. Bias voltage vs. Temperature

Forma prezentácie: poster