EXPERIMENTAL STUDY OF SPIN ANISOTROPY IN CutnCl2: A QUASI- TWO-DIMENSIONAL S = 1/2 SPATIALLY ANISOTROPIC TRIANGULAR-LATTICE ANTIFERROMAGNET

R. Tarasenko1, A. Orendáčová1, E. Čižmár1, M. Orendáč1, I. Potočňák2,  S. Zvyagin3

and A. Feher1

1Institute of Physics, Faculty of Science, P.J. Šafárik University, Park Angelinum 9, 041 54 Košice, Slovak Republic

2Institute of Chemistry, Faculty of Science, P.J. Šafárik University, Moyzesova 11, 0414 54 Košice, Slovak Republic

3Dresden High Magnetic Field Laboratory (HLD), Helmholtz-Zentrum Dresden-Rossendorf and TU Dresden, D-01314 Dresden, Germany

e-mail: robert.tarasenko@upjs.sk

Cu(tn)Cl2 has been previously identified as a potentional realization of a quasi-two-dimensional, spatially-anisotropic triangular Heisenberg antiferromagnet with spin 1/2, intralayer exchange coupling, J/kB ≈ -3 K, and interlayer exchange coupling, J´ ≈ 0.001 J. Electron paramagnetic resonance measurements of single crystals have been performed in the X-band range in the temperature range from 2 K to 300 K in magnetic fields up to 0.5 T. In the temperature range from 300 to 100 K g-factors  gc´ and ga´  change monotonously, there is a decrease of both components with decreasing temperature. However, at temperatures below 60 K significant increase of ga´ and decrease of gc´ was observed. This behaviour coincides with the theoretical predictions for the resonance fields in the presence of a dipolar coupling and the exchange anisotropy. The phonon modulation of the spin anisotropies can be responsible for the increase of the EPR linewidth observed above 100 K in both orientations. On the other hand, the upturn of the linewidth appearing below 20 K can be ascribed to the development of intralayer magnetic correlations.

This work was supported by the projects APVV LPP-0202-09, VEGA 1/0143/13 and ERDF EU project No. ITMS 26220120005.

Forma prezentácie: poster